IPC 6012 PWB COMPLIANCY FOR EVLA BASELINE

BOARD

CUSTOMER:		National Research Council/DRAO

PROJECT NAME:	IPC 6012 PWB Compliancy - EVLA Baseline Board

PROJECT NUMBER:	Z34-006223-55

This document has been approved by the following functions responsible for its implementation:

| Name | Title | Signature | Date |
| --- | --- | --- | --- |

| Revision History |  |  |  |
| --- | --- | --- | --- |
| Version | Date | Author (s) | Description of Change |
| 01 | April 27, 2009 | L. Zhu/L. Cutler | Initial Release |

CONFIDENTIAL INFORMATION

This is a confidential document that contains proprietary information and trade secrets of BreconRidge Corporation. No part of this document may be used, transmitted, reproduced or disclosed in any form or by any means without the prior written permission of BreconRidge Corporation.

Copyright © 2009 BreconRidge Corporation. All rights reserved.

TABLE OF CONTENTS

1	overview	5

1.1	Purpose	5

1.2	Reference documents	5

definitIOn of terms	5

1.3	5

2	Merix IPC 6012 compliance	6

3	Bow and Twist Measurement, Pre and Post SMT ASSEMBLY	10

3.1	MEthod	10

3.2	Test SETUP	11

3.3	Results	12

3.4	Discussion	16

4	IST TESTING	17

4.1	IST TESTING APPROACH	17

4.2	IST test condition	22

4.3	IST test Results	22

4.4	IST test Coupon cross section	28

5	conclusion and Qualification Status	32

TABLE OF TABLES

Table 1: Reference Documents	5

Table 2: Acronyms	5

Table 3: Merix Acceptance Testing and Frequency	6

Table 4  Test Equipment Detail	11

Table 5: Bow and Twist Testing Results	12

Table 6: IST Test Coupon Design	17

Table 7: Resistance Pre-screen Data for 0.028” DHS	18

Table 8:Resistance Prescreen Data for 0.0118” DHS	19

Table 9: Resistance Prescreen Data for 0.0098” DHS Blind Via for Layers 1-14	20

Table 10: Resistance Prescreen Data for 0.0098” DHS Blind Via for Layers 15-28	21

Table 11: IST Assembly Pre-conditioning	22

Table 12: IST Test Conditions	22

Table 13: IST Results for 0.028” DHS	23

Table 14: IST Results for 0.0118” DHS	23

Table 15: IST Results for 0.0098” DHS Blind Via for Layers 1-14	24

Table 16: IST Results for 0.0118” DHS Blind Via for Layers 15-28	24

TABLE OF FIGURES

Figure 1: Setup on CMM for twist measurement. Only 3 corners are constrained to the reference plane formed by the posts mounted to the press fit plate	11

Figure 2: Orientation for the Warp and Twist Measurement	12

Figure 3: Bow of Board 1 Pre and After Assembly, dimensions in mm.	13

Figure 4: Bow of Board 2 Pre and Post Assembly, dimensions in mm	14

Figure 5: Bow of Board 3 Pre and Post Assembly, dimensions in mm	15

Figure 6: Component PTH Assembly Conditioning: Ambient to 230°C for 6 IST cycles	25

Figure 7: Via PTH Assembly Conditioning: Ambient to 230°C for 6 IST cycles	26

Figure 8: Blind Via Layers 1-14 Assembly Conditioning: Ambient to 230°C for 6 IST cycles                 Drill Hole Size 0.0098”	27

Figure 9: Blind Via Layers 15-28 Assembly Conditioning: Ambient to 230°C for 6 IST cycles                 Drill Hole Size: 0.0098”	28

Figure 10  (A) PTH image of an untested coupon (B) PTH image of a tested coupon, 500 thermal cycles	29

Figure 11 (A) Via PTH image of an untested coupon   (B) Via PTH image of a tested coupon, , 500 thermal cycles	30

Figure 12 (A) Blind via (1-14) image of an untested coupon   (B) Blind via (1-14) image of a tested coupon, ,500 thermal cycles	31

Figure 13 (A) Blind via (15-28) image of an untested coupon   (B) Blind via (15-28) image of a tested coupon, , 500 thermal cycles	31

# overview

## Purpose

This document outlines the reliability engineering services that were conducted by BreconRidge Corporation (BreconRidge) for National Research Council for ELVA Baseline Board to qualify Merix Corporation, a new PWB supplier for the product.  The reliability work performed is in accordance with  STATEMENT OF WORK # 2 - IPC 6012 PWB COMPLIANCY – EVLA BASELINE BOARD.

This document summarises the testing results for the following information:

- Review of new PWB supplier’s compliance with IPC 6012 and test coverage

- Interconnect Stress Testing on one lot and review of data and cross sections

- Bow and twist of bare PWB board (3x parts), and as assembled CCA (3x parts)

## Reference documents

Table 1: Reference Documents

| Document number | Title |
| --- | --- |
| IPC-6012B | Qualification and Performance Specification for Rigid Printed Boards |
| IPC-TM-650 | Test Method Manual 2.4.22C Bow and Twist (Percentage) |
| IPC-TM-650 | Test Method Manual 2.6.26 DC Current Induce Thermal Cycling Test |
| SOW#2 | IPC 6012 PWB COMPLIANCY – EVLA BASELINE BOARD (November 24, 2008) |
| IPC-2221 | Generic Standard on Printed Board DesignI |

## definitIOn of terms

Table 2: Acronyms

| Term | Definition |
| --- | --- |
| BreconRidge | BreconRidge Corporation |
| NRC/DRAO | National Research Council/Dominion Radio Astrophysical Observatory |
| Merix | Merix Corporation |
| PWB | Printed Wiring Board |
| CCA | Circuit Card Assembly |
| IST | Interconnect Stress Test |
| AM | Asset Management |

# Merix IPC 6012 compliance

Merix demonstrates PWB manufacturing compliance with IPC 6012.  Table 3 is a summary outlining the acceptance criteria and frequency of the testing.

Table 3: Merix Acceptance Testing and Frequency

|  | IPC 6012 section | Performed on product first run (FAI) | Performed per product batch work order | Performed on sample basis | Other | Notes |
| --- | --- | --- | --- | --- | --- | --- |
| Inspection |  |  |  |  |  |  |
| Material | 3.2.1-3.2.14 | X | X |  |  |  |
| Visual |  |  |  |  |  |  |
| Edges of board | 3.3.1 | X | X |  |  |  |
| Laminate imperfections | 3.3.2 | X | X |  |  |  |
| Voids in plated hole | 3.3.3 | X | X |  |  |  |
| Lifted lands | 3.3.4 | X | X |  |  |  |
| Marking and traceability | 3.3.5 | X | X |  |  |  |
| Workmanship | 3.3.9 | X | X |  |  |  |
| Solderability |  |  |  |  |  |  |
| Surface/hole | 3.3.6 |  |  |  | X | Process Control |
| Dimensional |  |  |  |  |  |  |
| Board dimensional | 3.4 | X |  |  | X | Process control on production lot |
| Hole pattern accuracy | 3.4.1 | X | X |  |  |  |
| Pattern feature accuracy | 3.4.1 | X | X |  |  |  |
| Annular ring (external) | 3.4.2 | X | X |  |  |  |
| Bow and twist | 3.4.3 | X | X | X |  | Sample per lot |
| Solder resist coverage | 3.7-3.7.1 | X | X |  |  |  |
| Plating/coating thickness (electronic) | 3.6.2.11 | X | X | X |  | Sample per lot |
| Conductor Width |  |  |  |  |  |  |
| Internal | 3.5.1 | X | X |  |  |  |
| External | 3.5.1 | X | X |  |  |  |
| Conductor Spacing |  |  |  |  |  |  |
| Internal | 3.5.2 | X | X |  |  |  |
| External | 3.5.2 | X | X |  |  |  |
| Conductive Surfaces (Surface Only) |  |  |  |  |  |  |
| Edge board contact, junction of gold plate to solder finish | 3.3.8 | X | X |  |  |  |
| Nicks, dents, pinholes | 3.5.4.1 | X | X |  |  |  |
| Dewetting/nonwetting/final finish coverage | 3.5.4.5 3.5.4.6 3.5.4.7 | X | X |  |  |  |
| Edge board connector | 3.5.4.4 | X | X |  |  |  |
| Surface mount | 3.5.4.2 | X | X |  |  |  |
| Physical |  |  |  |  |  |  |
| Plating adhesion | 3.3.7 | X | X |  |  | Sample per lot |
| Solder resist cure and adhesion | 3.7 3.7.2 | X | X |  |  | Sample per lot |
| Structural Integrity After Stress Types 3-6 (Micro-section) |  |  |  |  |  |  |
| Plating integrity | 3.6.2.1 | X |  | X |  | If requested micro-section can be done per lot |
| Laminate voids | 3.6.2.3 | X |  |  |  |  |
| Etchback/negative etchback | 3.6 a & b 3.6.2.6 3.6.2.8 | X |  |  |  |  |
| Annular ring (internal) | 3.6 a & b 3.6.2.9 | X |  |  |  |  |
| Lifted lands | 3.6.2.10 | X |  |  |  |  |
| Hole plating thickness | 3.6 a & b 3.6.2.11 | X |  |  |  |  |
| Surface plating and conductor thickness | 3.6 a & b 3.6.2.11 3.6.2.13 | X |  |  |  |  |
| Conductor thickness (internal) | 3.6 a & b 3.6.2.12 | X |  |  |  |  |
| Metal core spacing | 3.6.2.14 | X |  |  |  |  |
| Dielectric thickness | 3.6 a & b 3.6.2.15 | X |  |  |  |  |
| Resin fill of blind/buried vias | 3.6.2.16 | X |  |  |  |  |
| Structural Integrity after Stress Types 2 (Micro-section) |  |  |  |  |  |  |
| Plating integrity | 3.6.2.1 | X |  |  |  | If requested micro-section can be done per lot |
| Laminate integrity | 3.6 a & b 3.6.2.3 | X |  |  |  |  |
| Lifted lands | 3.6.2.10 | X |  |  |  |  |
| Hole plating thickness | 3.6 a & b 3.6.2.11 | X |  |  |  |  |
| Surface plating and conductor thickness | 3.6 a & b 3.6.2.11 3.6.2.13 | X |  |  |  |  |
| Electrical |  |  |  |  |  |  |
| Circuit continuity | 3.8.2.1 | X | X |  |  |  |
| Insulation resistance | 3.8.2.2 | X | X |  |  |  |
| Cleanliness |  |  |  |  |  |  |
| Cleanliness prior to solder resist application | 3.9.1 |  |  |  | X | Process control |
| Special Requirements (when specified) |  |  |  |  |  |  |
| Metal core (horizontal micro-section) | 3.10.10 |  |  |  |  | As requested |
| Solder resist thickness | 3.7.3 |  |  |  |  |  |
| Dielectric withstanding voltage | 3.8.1 |  |  |  |  |  |
| Circuit/plated-through shorts to metal substrate | 3.8.3 |  |  |  |  |  |
| Cleanliness after surface coating application | 3.9.2 |  |  |  |  |  |
| Cleanliness of inner layers after oxide treatment prior to lamination | 3.9.3 |  |  |  |  |  |
| Outgassing | 3.10.1 |  |  |  |  |  |
| Organic contamination | 3.10.2 |  |  |  |  |  |
| Fungus resistance | 3.10.3 |  |  |  |  |  |
| Vibration | 3.10.4 |  |  |  |  |  |
| Mechanical shock | 3.10.5 |  |  |  |  |  |
| Impedance testing | 3.10.6 | X | X | X |  | Sample per lot |
| Coefficient of thermal expansion | 3.10.7 |  |  |  |  | As requested |
| Thermal shock | 3.10.8 | X |  |  |  |  |
| Surface insulation resistance (as received) | 3.10.9 |  |  |  |  | As requested |
| Repair | 3.11 |  |  |  |  |  |
| Circuit repair | 3.11.1 |  |  |  |  |  |

Specific data for the Baseline board builds has been provided by Merix as supporting data and will be forwarded to NRC/DRAO with this document. The data is summarized in an Excel file named “Summary for IPC6012 Compliance for Baseline Board” which is provided to NRC with the repot together.

Additional testing to be performed on the Baseline Board include bow and twist measurements (pre and post SMT) and IST testing.  The results of this testing will be covered in the following sections.

# Bow and Twist Measurement, Pre and Post SMT ASSEMBLY

## MEthod

The IPC-TM-650 Test Method 2.4.22C was used to measure the bow and twist of the baseline boards, pre and post SMD assembly. Normal methods for Bow and Twist would use a reference plane with the bow and twist being measured relative to this.  For Bow measurements, 2 opposite edges are constrained against the horizontal reference plane.  Although, this technique could have been used for the bare PWBs, this would not have been possible with the assembled boards due to the interference of the components on the board. Also, due to the size and weight of the baseline boards, significant deflection takes place due to self-weight which will affect both the bow and twist results if the IPC method was used as is.  An alternate method was devised to reduce significantly the effect of self weight and yet give a good estimate of the bow and twist that is occurring. The measurements were done on a CMM (coordinate measurement machine) with the PWB’s on edge and measured relative to reference plane mounted vertically as well. The measurement method follows.

- Four points on the reference plane were measured. These points were used to define a reference plane using coordinate geometry. In this way any errors in alignment of the reference plane to the coordinate system of the CMM can be compensated for.

- The baseline boards were mounted on this reference plane. Three corners were fixed to this reference plane for twist measurements and four corners were fixed for bow measurements.

- Data collected was analysed in a spreadsheet that calculated the deviations from the reference plane. Bow measurements were done in a grid pattern in order to find the maximum in bow relative to the reference plane. The bow was calculated relative to the lowest point measured.

The bow is calculated as follows:

BL=RLL×100           Bw=RwW×100

Where:

BL = Percentage bow in the length direction

BW = Percentage bow in the width direction

RL = Measured maximum feeler/pin gauge size across sample length

RW = Measured maximum feeler/pin gauge size across sample width

L = Length measurement as determined above

W = Width measurement as determined above

The twist is calculated as follows:

PercentageTwist=R2(D)×100

Where:

R = Go/No-Go feeler/pin gauge size

D = Diagonal measurement across the sample as determined above

Note: This formula includes a factor of two because, by constraining one corner of the sample, the vertical deflection of twist is approximately doubled.

## Test SETUP

The test setup is shown in Figure 1.  The reference plane was a modified form of the press fit plate. This photo is for a twist measurement.  Note the distance between the PWB and the reference plane (pin at corner of the press fit adapter where board is not touching). This is 2 times the twist value. On the Coordinate Measurement Machine (CMM) the X, Y and Z axis correspond to the Z, X and Y axis on the PWB being measured.

Figure 1: Setup on CMM for twist measurement. Only 3 corners are constrained to the reference plane formed by the posts mounted to the press fit plate

Table 4  Test Equipment Detail

| Description | Model | Manufacturer | Equip. Serial Number | AM Number | Calibration Valid (MM/DD/YY) | Location of Equipment |
| --- | --- | --- | --- | --- | --- | --- |
| Coordinate Measurement Machine | B-241 | Mitutoyo | 8405276 (unit) 3010346 (counter) | CMM-1 | 03/05/2010 | Breconridge |

## Results

The limit for both bow and twist is 0.75% for surface mount PWBs per IPC 2221.  The same guideline was used for the assembled CCA even though IPC 2221 applies only to bare PWB’s. Any boards that exceed this limit are highlighted in red text in the following table. Some of the Pre-SMT and post-SMT bow and twist values are higher than expected.  The Post-SMT specification is a guideline but care should be taken when clamping the boards into the system to ensure minimum stress is projected onto the solder joints of the components.

The bow measurements were done using the following orientation of the PWB.  The NRC-CNRC label is on the opposite side.  The positive X direction is towards the right.

Figure 2: Orientation for the Warp and Twist Measurement

For all three boards the twist improved after assembly. Even the board 2 which had excessive twist prior to assembly had acceptable twist after assembly.

Three dimensional plots of the bow measurements before and after assembly are shown in Figures 3 to 5. Prior to assembly, all three boards had acceptable bow. Boards 1 and 3 had a convex shape whereas Board 2 and a concave shape. After assembly the initial shapes where exaggerated with the bow increasing for all three boards. The amount of bow exceeded the desired limit for both Boards 3 and 1 and was close to the limit for Board 2. It must be remembered that this is only a recommendation and not a hard requirement after assembly.

Table 5: Bow and Twist Testing Results

| Board | Assembly Status | Spec. | Bow |  | Twist |
| --- | --- | --- | --- | --- | --- |
|  |  |  | RL | Rw |  |
| Board1 | Pre-SMT | 0.75% | 0.45% | 0.57% | 0.38% |
|  | Post-SMT | 0.75% | 0.70% | 0.88% | 0.09% |
| Board2 | Pre-SMT | 0.75% | 0.30% | 0.38% | 0.85% |
|  | Post-SMT | 0.75% | 0.57% | 0.72% | 0.35% |
| Board3 | Pre-SMT | 0.75% | 0.31% | 0.39% | 0.38% |
|  | Post-SMT | 0.75% | 0.79% | 0.99% | 0.15% |

Figure 3: Bow of Board 1 Pre and After Assembly, dimensions in mm.

Figure 4: Bow of Board 2 Pre and Post Assembly, dimensions in mm

Figure 5: Bow of Board 3 Pre and Post Assembly, dimensions in mm

## Discussion

The as-received PWB’s meet the IPC 2221 specifications for bow for all three boards and twist for 2 out of 3 boards. The excessive twist did not seem to cause a problem during assembly as all the assembled boards had acceptable twist after assembly.

The increase in bow after SMT may induce an increase the stress in the BGA solder joints when the board assembly is fastened into the chassis. This should be kept in mind when evaluating the overall assembly. The acceptable bow after SMT depends upon the end application and next level assembly.

The source of this increased bow is not clear as it seems to be related to the initial shape of the PWB prior to SMT assembly.  The stress states of the assembled PWB is very complex with the PWB stackup, imbalance in the component density on both side of the PWB and the supporting framework during SMT reflow all playing a role.

# IST TESTING

## IST TESTING APPROACH

Interconnect stress testing (IST) is a relatively new method to determine the resistance of both plated through hole and via interconnect to temperature cycling. A controlled DC current is used to self heat the daisy chained interconnect on specially designed coupons that represent the PWB technology being evaluated. By increasing and decreasing the current in the circuit, the temperature of the PWB can be cycled between ambient and the maximum test temperature, typically 150°C.  During the maximum temperature excursions interconnect electrical resistances are monitored. Increases in resistance indicate the development of cracking in the interconnect structure. Typically resistance increases of about 10% are considered as failures.

Prior to the beginning of the IST testing phase, the IST coupons are pre-tested by heating to 230°C for six cycles to simulate the conditions that the boards undergo at assembly process.

IST testing was performed by on 24 coupons to represent the same via structures as found in the baseline board design. The coupon designs for the component PTH, via PTH, and blind vias are detailed in Table 5

Table 6: IST Test Coupon Design

| PTH Type | Layers | Drill Diameter | Pad Diameter | Pitch Between Holes | Notes |
| --- | --- | --- | --- | --- | --- |
| Component PTH | 1-28 | 0.028” AR: 4.5 | 0.0394” | 0.075” | Single Sense design |
| Via PTH | 1-28 | 0.0118” AR: 10.7 | 0.0218” | 0.033” | Single Sense design |
| Blind Via | 1-14 | 0.0098” AR: 6.1 | 0.0218” | 0.033” | Single Sense design |
| Blind Via | 15-28 | 0.0098” AR: 6.1 | 0.0218” | 0.033” | Single Sense design |

AR [=] Aspect Ratio

The resistance data for the IST coupons are detailed in Table 7 to 10 below. The rows highlighted were IST coupons that were chosen for stress testing, these coupons typically were close to the mean resistance for all of the coupons.  Note the tight distribution in resistance values indicating good process control in the manufacture of the coupons. The acronym DHS stands for Drilled Hole Size (Drilled Hole Diameter).

Table 7: Resistance Pre-screen Data for 0.028” DHS

| Coupon ID. | Post Resistance | PTH Resistance |
| --- | --- | --- |
| 1281 | 616 | 239 |
| 1282 | 621 | 241 |
| 1283 | 617 | 241 |
| 1284 | 622 | 241 |
| 1285 | 622 | 239 |
| 1286 | 622 | 241 |
| 1287 | 619 | 240 |
| 1288 | 617 | 239 |
| 1289 | 619 | 241 |
| 12810 | 618 | 240 |
| 12811 | 618 | 241 |
| 12812 | 621 | 241 |
| 2281 | 618 | 240 |
| 2282 | 619 | 241 |
| 2283 | 619 | 241 |
| 2284 | 621 | 241 |
| 2285 | 622 | 240 |
| 2286 | 623 | 242 |
| 2287 | 623 | 241 |
| 2288 | 619 | 239 |
| 2289 | 619 | 242 |
| 22810 | 621 | 241 |
| 22811 | 619 | 241 |
| 22812 | 623 | 240 |
| 3281 | 617 | 240 |
| 3282 | 617 | 238 |
| 3283 | 622 | 240 |
| 3284 | 622 | 241 |
| 3285 | 620 | 239 |
| 3286 | 618 | 239 |
| 3287 | 617 | 239 |
| 3288 | 621 | 239 |
| 3289 | 624 | 241 |
| 32810 | 621 | 239 |
| 32811 | 619 | 240 |
| 32812 | 620 | 240 |
| Mean | 619.9 | 240.2 |
| StDev | 2.12 | 0.99 |
| Min | 616 | 238 |
| Max | 624 | 242 |
| Range | 8 | 4 |

Table 8:Resistance Prescreen Data for 0.0118” DHS

| Coupon ID. | Post Resistance | PTH Resistance |
| --- | --- | --- |
| 1121 | 716 | 422 |
| 1122 | 704 | 418 |
| 1123 | 710 | 420 |
| 1124 | 708 | 420 |
| 1125 | 713 | 423 |
| 1126 | 710 | 417 |
| 1127 | 710 | 422 |
| 1128 | 716 | 422 |
| 1129 | 720 | 417 |
| 11210 | 720 | 419 |
| 11211 | 712 | 421 |
| 11212 | 704 | 417 |
| 2121 | 710 | 417 |
| 2122 | 711 | 418 |
| 2123 | 716 | 418 |
| 2124 | 714 | 419 |
| 2125 | 708 | 414 |
| 2126 | 704 | 415 |
| 2127 | 713 | 417 |
| 2128 | 709 | 416 |
| 2129 | 715 | 420 |
| 21210 | 711 | 415 |
| 21211 | 712 | 420 |
| 21212 | 710 | 424 |
| 3121 | 709 | 409 |
| 3122 | 709 | 411 |
| 3123 | 709 | 417 |
| 3124 | 712 | 412 |
| 3125 | 710 | 414 |
| 3126 | 707 | 413 |
| 3127 | 711 | 416 |
| 3128 | 712 | 410 |
| 3129 | 713 | 410 |
| 31210 | 717 | 412 |
| 31211 | 712 | 410 |
| 31212 | 715 | 412 |
| Mean | 711.6 | 416.6 |
| StDev | 3.69 | 4.08 |
| Min | 704 | 410 |
| Max | 720 | 423 |
| Range | 16 | 13 |

Table 9: Resistance Prescreen Data for 0.0098” DHS Blind Via for Layers 1-14

| Coupon ID. | Post Resistance | PTH Resistance |
| --- | --- | --- |
| 1101 | 769 | 346 |
| 1102 | 767 | 347 |
| 1103 | 774 | 350 |
| 1104 | 768 | 346 |
| 1105 | 773 | 342 |
| 1106 | 774 | 344 |
| 1107 | 782 | 346 |
| 1108 | 772 | 343 |
| 1109 | 770 | 346 |
| 11010 | 774 | 340 |
| 11011 | 778 | 344 |
| 11012 | 772 | 345 |
| 2101 | 757 | 333 |
| 2102 | 778 | 344 |
| 2103 | 775 | 345 |
| 2104 | 773 | 344 |
| 2105 | 771 | 343 |
| 2106 | 765 | 339 |
| 2107 | 773 | 343 |
| 2108 | 775 | 342 |
| 2109 | 767 | 339 |
| 21010 | 769 | 342 |
| 21011 | 762 | 337 |
| 21012 | 778 | 340 |
| 3101 | 773 | 346 |
| 3102 | 773 | 345 |
| 3103 | 785 | 349 |
| 3104 | 782 | 346 |
| 3105 | 779 | 342 |
| 3106 | 782 | 348 |
| 3107 | 782 | 347 |
| 3108 | 780 | 345 |
| 3109 | 775 | 343 |
| 31010 | 773 | 344 |
| 31011 | 775 | 349 |
| 31012 | 775 | 347 |
| Mean | 773.6 | 343.9 |
| StDev | 5.91 | 3.50 |
| Min | 757 | 333 |
| Max | 785 | 350 |
| Range | 28 | 17 |

Table 10: Resistance Prescreen Data for 0.0098” DHS Blind Via for Layers 15-28

| Coupon ID. | Post Resistance | PTH Resistance |
| --- | --- | --- |
| 1101 | 777 | 362 |
| 1102 | 769 | 359 |
| 1103 | 765 | 354 |
| 1104 | 768 | 355 |
| 1105 | 764 | 353 |
| 1106 | 772 | 356 |
| 1107 | 765 | 354 |
| 1108 | 762 | 352 |
| 1109 | 765 | 354 |
| 11010 | 771 | 356 |
| 11011 | 765 | 354 |
| 11012 | 766 | 354 |
| 2101 | 765 | 350 |
| 2102 | 771 | 355 |
| 2103 | 769 | 353 |
| 2104 | 772 | 353 |
| 2105 | 766 | 350 |
| 2106 | 768 | 350 |
| 2107 | 767 | 349 |
| 2108 | 770 | 351 |
| 2109 | 771 | 358 |
| 21010 | 771 | 354 |
| 21011 | 782 | 360 |
| 21012 | 767 | 351 |
| 3101 | 771 | 354 |
| 3102 | 765 | 350 |
| 3103 | 767 | 355 |
| 3104 | 777 | 362 |
| 3105 | 774 | 356 |
| 3106 | 765 | 348 |
| 3107 | 765 | 348 |
| 3108 | 765 | 350 |
| 3109 | 762 | 349 |
| 31010 | 766 | 349 |
| 31011 | 770 | 353 |
| 31012 | 766 | 351 |
| Mean | 768.4 | 353.4 |
| StDev | 4.36 | 3.66 |
| Min | 762 | 348 |
| Max | 782 | 362 |
| Range | 20 | 14 |

## IST test condition

The 24 selected coupons were exposed to IST Assembly Conditioning per Table 11 and IST Test parameters per Table 12.

Table 11: IST Assembly Conditioning

| Number of IST Cycles | 6 |
| --- | --- |
| Test Temperature | 230C |
| Compensation | Yes |
| Precycle Time Window | 3 seconds |
| % Reject Power | 10 |

Table 12: IST Test Conditions

| Number of IST Cycles | 500 |
| --- | --- |
| MaxTest Temperature | 150C |
| Min. Test Temperature | 25°C |
| Delta Temperature | 125°C |
| Data Recorded Every ? Cycles | 25 |
| Compensation | Yes |
| Pre-cycle Time Window | 3 seconds |
| % Reject Power | 10 |
| % Reject Sense | 10 |

## IST test Results

No failures were found during IST testing. There was negligible change in the resistance values for all 4 test coupon types evaluated. This indicates that little or no cracking occurred during the stress testing.

The tabulated IST results are in Table 13 to 16.  The resistance change graphs are in Figures 6 to 9.

Table 13: IST Results for 0.028” DHS

| Test Condition | Coupon ID | Post Cycles | Post % | PTH Cycles | PTH % | Failure Mode |
| --- | --- | --- | --- | --- | --- | --- |
| 6X@230C | 1282 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 12811 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 2286 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 2289 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 3284 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 3289 | 500 | 0.0 | 500 | 0.0 | No Failure |
| Mean |  | 500 | 0.0 | 500 | 0.0 | All Suspend Data |
| StDev |  | 0.0 | 0.0 | 0.0 | 0.0 |  |
| Min |  | 500 | 0.0 | 500 | 0.0 |  |
| Max |  | 500 | 0.0 | 500 | 0.0 |  |
| Range |  | 0 | 0.0 | 0 | 0.0 |  |

Table 14: IST Results for 0.0118” DHS

| Test Condition | Coupon ID | Post Cycles | Post % | PTH Cycles | PTH % | Failure Mode |
| --- | --- | --- | --- | --- | --- | --- |
| 6X@230C | 1125 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 1128 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 21211 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 21212 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 3123 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 3127 | 500 | 0.0 | 500 | 0.0 | No Failure |
| Mean |  | 500 | 0.0 | 500 | 0.0 | All Suspend Data |
| StDev |  | 0.0 | 0.0 | 0.0 | 0.0 |  |
| Min |  | 500 | 0.0 | 500 | 0.0 |  |
| Max |  | 500 | 0.0 | 500 | 0.0 |  |
| Range |  | 0 | 0.0 | 0 | 0.0 |  |

Table 15: IST Results for 0.0098” DHS Blind Via for Layers 1-14

| Test Condition | Coupon ID | Post Cycles | Post % | PTH Cycles | PTH % | Failure Mode |
| --- | --- | --- | --- | --- | --- | --- |
| 6X@230C | 1103 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 1109 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 2103 | 500 | 0.0 | 500 | 0.1 | No Failure |
| 6X@230C | 2107 | 500 | 0.2 | 500 | 0.1 | No Failure |
| 6X@230C | 3103 | 500 | 0.1 | 500 | 0.0 | No Failure |
| 6X@230C | 31011 | 500 | 0.2 | 500 | 0.2 | No Failure |
| Mean |  | 500 | 0.08 | 500 | 0.07 | All Suspend Data |
| StDev |  | 0.0 | 0.04 | 0.0 | 0.03 |  |
| Min |  | 500 | 0.0 | 500 | 0.0 |  |
| Max |  | 500 | 0.2 | 500 | 0.2 |  |
| Range |  | 0 | 0.2 | 0 | 0.2 |  |

Table 16: IST Results for 0.0118” DHS Blind Via for Layers 15-28

| Test Condition | Coupon ID | Post Cycles | Post % Resistance Change | PTH Cycles | PTH % | Failure Mode |
| --- | --- | --- | --- | --- | --- | --- |
| 6X@230C | 1101 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 1102 | 500 | 0.0 | 500 | 0.2 | No Failure |
| 6X@230C | 2109 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 21011 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 3104 | 500 | 0.0 | 500 | 0.0 | No Failure |
| 6X@230C | 3105 | 500 | 0.0 | 500 | 0.1 | No Failure |
| Mean |  | 500 | 0.0 | 500 | 0.05 | All Suspend Data |
| StDev |  | 0.0 | 0.0 | 0.0 | 0.08 |  |
| Min |  | 500 | 0.0 | 500 | 0.0 |  |
| Max |  | 500 | 0.0 | 500 | 0.2 |  |
| Range |  | 0 | 0.0 | 0 | 0.2 |  |

Figure 6: Component PTH Assembly Conditioning: Ambient to 230°C for 6 IST cycles

Figure 7: Via PTH Assembly Conditioning: Ambient to 230°C for 6 IST cycles

Figure 8: Blind Via Layers 1-14 Assembly Conditioning: Ambient to 230°C for 6 IST cycles
                Drill Hole Size 0.0098”

Figure 9: Blind Via Layers 15-28 Assembly Conditioning: Ambient to 230°C for 6 IST cycles
                Drill Hole Size: 0.0098”

## IST test Coupon cross section

Crosse section analysis was conducted on both untested and tested IST coupons. The PTHs and vias of all four types of coupons were evaluated. Little difference was found between the untested and thermally cycled coupons. No barrel cracks or cracking at surface lands or inner layers were detected.  This confirms the results of the IST resistance measurements. Cross-section images are shown in Figure 10 to Figure 13.

.

Figure 10  (A) PTH image of an untested coupon (B) PTH image of a tested coupon, 500 thermal cycles

Figure 11 (A) Via PTH image of an untested coupon   (B) Via PTH image of a tested coupon, , 500 thermal cycles

Figure 12 (A) Blind via (1-14) image of an untested coupon   (B) Blind via (1-14) image of a tested coupon, ,500 thermal cycles

Figure 13 (A) Blind via (15-28) image of an untested coupon   (B) Blind via (15-28) image of a tested coupon, , 500 thermal cycles

# conclusion

- The IPC testing performed by Merix and data demonstrates their PWB manufacturing compliance to IPC 6012.

- The Merix boards had acceptable as-received bow and only slightly exceed the twist limit for one out of three PWB’s (IPC 2221). This did not cause any issues during SMT assembly.

- After SMT assembly, the bow did increase. Whether this will have negative impact will have to be determined at the next level assembly.  If this does prove to be an issue, further evaluation of the board design and SMT assembly process will be required.

- IST testing was performed on four types of IST coupons which included PTH, via and blind via structures. These coupons use the same drill sizes and PWB stack-up that was used for the Baseline board manufacture. No failures, significant resistance changes or interconnect cracking were found during or after testing. These results demonstrate the robustness of the PWB technology used to manufacture the Baseline boards.